COATING (PAINT) SPECIFICATION SHEET

R/V MEDEIA

PPG / Ameron Protective & Marine Coatings

| Vessel | R/V Medeia | Date | August 7, 2026 |
| --- | --- | --- | --- |
| Coating supplier | PPG / Ameron (PMC) | Spec rev. | Draft 1 |
| Application method | Airless spray (brush/roll for stripe & touch-up) | DFT gauge | Per SSPC-PA 2 |

# 1.  Scope

Covers surface preparation and coating build for the R/V Medeia across two service environments: (A) above-waterline atmospheric surfaces — hull topsides, superstructure/deckhouse, and weather decks; and (B) below-waterline immersed surfaces — the bottom / underwater hull. All preparation, mixing, thinning, application, and cure shall conform to the current PPG/Ameron Product Data Sheets (PDS), which govern in case of conflict with this summary.

Product identification note: “Ameron 302” is specified here as Dimetcote 302 H (Ameron/PPG reinforced inorganic-zinc primer) — PPG’s zinc-primer line. Confirm before issue if a different product was intended.

# 2.  Surface Preparation Standards

Governing rule: surface preparation follows the minimum requirements of the applicable Ameron PDS. Solvent-clean all surfaces to SSPC-SP1 (remove oil, grease, salts) before any mechanical prep. Remove weld spatter, round sharp edges, and grind smooth per SSPC-SP2/SP3 as needed.

| Condition | Standard (per Ameron PDS minimum) |
| --- | --- |
| Bare mild steel above waterline (under Dimetcote 302 H) | SSPC-SP6 / NACE No. 3 (Commercial Blast) minimum; angular anchor profile 1.5–3.0 mils (5.0 mils max). Near-white SSPC-SP10 recommended on new steel for best service life. |
| Bare mild steel below waterline (under Amercoat 235, immersion) | SSPC-SP10 / NACE No. 2 (Near-White Blast); angular anchor profile 2.0–4.0 mils — required for immersion / tank-lining service per Amercoat 235 PDS. |
| Disturbed / damaged / previously-coated areas | SP1 solvent-clean, then restore to the original prep standard by spot abrasive blast where feasible. Where blasting is not feasible, power-tool clean to bare metal to SSPC-SP11 (produces a surface profile). Feather / abrade the edges of surrounding sound coating and remove all dust and residue before recoating. |

# 3.  Application & Environmental Conditions

- Substrate temperature at least 5°F (3°C) above the dew point and rising during application and cure.

- Relative humidity below 85%; do not apply to damp or contaminated surfaces.

- Observe each product’s minimum/maximum application and substrate temperatures per its PDS. Dimetcote 302 H (inorganic zinc) requires ambient moisture to cure fully before topcoating.

- Verify DFT of each coat per SSPC-PA 2 before applying the next.

# 4.  System A — Above-Waterline (Topsides, Superstructure, Decks)

| # | Coat / Step | Product | Generic Type | DFT/coat (mils) | Notes |
| --- | --- | --- | --- | --- | --- |
| 1 | Primer (DTM) | Dimetcote 302 H | Inorganic zinc | 2.0–4.0 (3.0 target) | Applied direct to prepared bare steel. |
| 2 | Stripe / mist-tie coat | Amercoat 235 | Phenalkamine epoxy | Brush (not in nominal DFT) | Brush-apply to welds, edges, corners, bolt heads. Mist-coat/full-coat technique over the inorganic zinc to minimize bubbling/pinholing (per 235 PDS). |
| 3 | Intermediate coat 1 | Amercoat 235 | Phenalkamine epoxy | 4.0–6.0 | Color A. |
| 4 | Intermediate coat 2 | Amercoat 235 | Phenalkamine epoxy | 4.0–6.0 | Color B — contrasting with Color A for full-coverage verification. |
| 5 | Finish coat 1 | PSX 700 | Engineered siloxane | 3.0–5.0 | Per finish color schedule. |
| 6 | Finish coat 2 | PSX 700 | Engineered siloxane | 3.0–5.0 | Final finish color. |

Nominal system DFT: approx. 16–24 mils (excluding stripe coat).

Recoat windows (≈70–75°F): Dimetcote 302 H — min 1.5 h, max 3 months (power-wash before topcoating). Amercoat 235 — min 4 h, max 30 days over itself (abrade if exceeded). PSX 700 — min 3 h (20°C), max unlimited.

# 5.  System B — Below-Waterline (Bottom / Underwater Hull)

Do NOT use inorganic zinc (Dimetcote 302 H) below the waterline or under antifouling. Zinc-silicate primers are not recommended for continuous immersion beneath antifoulings. Use an epoxy anticorrosive barrier (Amercoat 235), which is an approved undercoat for ABC 3 antifouling.

| # | Coat / Step | Product | Generic Type | DFT/coat (mils) | Notes |
| --- | --- | --- | --- | --- | --- |
| 1 | Stripe coat | Amercoat 235 | Phenalkamine epoxy | Brush (not in nominal DFT) | Brush edges, welds, and seams before full coats. |
| 2 | Anticorrosive 1 | Amercoat 235 | Phenalkamine epoxy | 4.0–6.0 | Color A. Applied to near-white blasted steel. |
| 3 | Anticorrosive 2 | Amercoat 235 | Phenalkamine epoxy | 4.0–6.0 | Color B — contrasting for coverage verification. |
| 4 | Antifouling 1 | ABC 3 | Tin-free self-polishing antifouling | 4.0–6.0 | Over cured Amercoat 235 (within 235 max recoat, or abrade). |
| 5 | Antifouling 2 | ABC 3 | Tin-free self-polishing antifouling | 4.0–6.0 | Contrasting / signal color. |

Nominal system DFT: approx. 16–24 mils (excluding stripe coat).

Recoat windows (≈70–75°F): Amercoat 235 — min 4 h. ABC 3 — min 5 h over itself; over 235 within the 235 maximum recoat window (abrade if exceeded). Observe launch (dry-to-immersion) time per the ABC 3 PDS.

Boottop / waterline band: use the Amercoat 235 anticorrosive with an appropriate atmospheric finish (PSX 700), or a dedicated boottop finish, per the yard’s color scheme.

# 6.  General Notes

- Colors: the two Amercoat 235 coats (and the two ABC 3 coats) shall be applied in contrasting/alternating colors so each coat’s coverage can be visually verified. Final PSX 700 finish colors per the vessel color schedule.

- Decks & walking surfaces: where non-skid is required, incorporate an approved aggregate in the intermediate/finish coat or use a dedicated non-skid system — specify separately.

- Mixing ratios, induction time, pot life, thinning, and cure/launch times shall follow the current PPG/Ameron PDS for each product.

- DFT measured per SSPC-PA 2; keep application records (ambient conditions, DFT, batch numbers) for the coating log.

# 7.  Manufacturer References

- PPG Dimetcote 302 H — Product Data Sheet (reinforced inorganic zinc primer).

- PPG Amercoat 235 — Product Data Sheet, May 1, 2018 (phenalkamine epoxy).

- PPG PSX 700 — Product Data Sheet, Nov 6, 2023 (engineered siloxane).

- PPG ABC 3 — Product Data Sheet, May 1, 2018 (tin-free self-polishing antifouling).

This specification summarizes manufacturer data for bid/planning use. The current PPG/Ameron Product Data Sheets and Application Instructions govern all work.